## Slide 1: The Effects of Pressure and Bending on Steel Pipe
P.R. Underhill, T.W. Krause, S. Chaudhury
Royal Military College of Canada

## Slide 2
Motivation
Background
Experimental Set Up
Results
Conclusions
Outline
2

## Slide 3
Motivation
Magnetic Metal Memory
3

## Slide 4
Background
4
Notes: Ferromagnetic materials are organized into magnetic domains that are aligned with the <100> directions
Lowest energy state is flux closure.

## Slide 5
Background
5
Notes: Application of an external field causes domains aligned with the field to grow
Application of stress causes growth of domains aligned with stress to grow. domain refinement. Villari effect

## Slide 6
Background
Pinning prevents domain wall motion
MBN suggests not much domain wall motion below 0.1T
Earth’s field 53 mT in Kingston
6
Notes: Application of an external field causes domains aligned with the field to grow
Application of stress causes growth of domains aligned with stress to grow. domain refinement. Villari effect

## Slide 7
Questions
How can MMM work?
How does the earth’s field interact with steel structures?
How much does stress affect the magnetization of pipes?
How reproducible/quantifiable are the effects?
7

## Slide 8
Experiments
 | 1 | 2 | 3
OD (cm) | 3.3 | 3.3 | 9.1
ID (cm) | 2.54 | 2.54 | 8.9
Thickness (mm) t | 3.8 | 3.8 | 5.4
Length (m) | 0.95 | 3.14 | 0.95
Manufacture | extruded | extruded | rolled
Hoop stress (MPA)/ Internal P (ksi) | 27 | 27 | 55
1
2
3
8

## Slide 9
Experiments
Z
Z
Z
Y
Y
Y
Tubes 1 and 2
radial  1.06 mT
Tube 3
Scanner
X Axial  0.1 mT
Y Radial  0.1 mT
9

## Slide 10
Results – Rotation in Earth’s Field
Chart: Radial Magnetic Field (uT)
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90
0 | -154.0044 | -123.0358 | -101.644 | -83.2265 | -66.0714 | -49.0881 | -33.9262 | -18.8593 | -3.1056 | 12.8748 | 27.2894 | 44.8629 | 59.4201 | 77.3332 | 95.6503 | 114.3437 | 136.574 | 163.7809
45 | -140.5544 | -112.9894 | -93.7954 | -75.5734 | -59.0815 | -43.2071 | -28.5897 | -14.2335 | 0.12635 | 13.5507 | 26.9551 | 40.4033 | 54.6937 | 68.5968 | 84.8311 | 102.061 | 123.577 | 151.4143
90 | -122.716 | -101.3663 | -87.9346 | -73.4176 | -53.0727 | -40.7554 | -26.7719 | -15.1561 | -1.0996 | 13.1014 | 24.5308 | 37.9552 | 52.0939 | 66.7077 | 81.3251 | 99.1873 | 115.6006 | 138.4503
135 | -98.319 | -88.3913 | -78.3851 | -65.0483 | -53.491 | -40.105 | -26.6659 | -15.1342 | -0.88215 | 12.7724 | 23.7141 | 36.4224 | 49.2987 | 61.8169 | 74.1307 | 86.7001 | 101.2152 | 114.7327
180 | -96.7752 | -81.4964 | -68.7388 | -56.1748 | -46.2983 | -32.3642 | -21.0718 | -9.6242 | 1.8692 | 14.1756 | 23.767 | 34.9827 | 45.5735 | 58.1028 | 71.4724 | 80.3825 | 92.6687 | 101.6372
225 | -97.2757 | -86.4437 | -75.6319 | -62.8195 | -52.013 | -38.51 | -25.8182 | -13.8736 | -0.5003 | 12.8931 | 23.8164 | 35.0211 | 46.4925 | 58.6472 | 72.2288 | 82.626 | 93.6882 | 104.0926
270 | -110.9358 | -94.581 | -80.1755 | -66.667 | -54.9819 | -42.6024 | -29.0995 | -16.5739 | -4.4264 | 9.8128 | 21.0796 | 34.0254 | 47.0242 | 61.4954 | 75.6963 | 89.2231 | 105.2381 | 122.5174
315 | -130.3801 | -107.9689 | -88.4662 | -72.0036 | -57.7807 | -42.8619 | -29.5379 | -15.9929 | -3.0708 | 9.2026 | 22.0862 | 34.5899 | 47.0479 | 60.7866 | 77.0355 | 93.9256 | 114.8991 | 147.3019
Degaussed at 0
Pipe #1
North
degauss
measure
10

## Slide 11
Results – Degauss direction
Chart: Distance (cm)
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90
0 | 82.2277 | 73.82 | 66.388 | 55.6346 | 45.2411 | 34.5424 | 21.7483 | 9.9937 | -0.6794 | -11.1844 | -19.7619 | -29.0008 | -37.2366 | -46.556 | -53.6354 | -60.6362 | -67.6993 | -76.4997
45 | 82.9676 | 73.3067 | 63.0356 | 50.1975 | 38.6348 | 25.2359 | 12.4765 | 1.2609 | -8.9244 | -17.734 | -25.3852 | -31.1912 | -37.2294 | -43.1724 | -47.9371 | -51.0941 | -55.254 | -57.609
90 | -23.8981 | -17.7395 | -14.2262 | -13.2707 | -13.0168 | -12.2294 | -11.9608 | -12.8231 | -11.9298 | -11.0583 | -8.9536 | -4.4923 | -1.1672 | 5.5341 | 13.1323 | 23.3908 | 35.6989 | 53.4422
135 | -86.2191 | -66.8954 | -54.3735 | -44.9994 | -36.0601 | -28.0014 | -20.9676 | -14.7688 | -8.5298 | -2.3437 | 4.7138 | 13.0392 | 21.3098 | 32.1217 | 44.651 | 58.7805 | 77.6274 | 102.8448
180 | -122.8256 | -106.427 | -95.7027 | -87.1362 | -73.5126 | -60.5832 | -46.4975 | -29.9928 | -13.0899 | 3.424 | 19.6345 | 35.7756 | 52.0884 | 67.8862 | 84.3908 | 99.2549 | 116.969 | 143.8726
225 | -88.0697 | -76.9582 | -69.3508 | -64.5422 | -55.8642 | -48.1106 | -38.7658 | -27.6488 | -16.245 | -4.5854 | 7.9585 | 21.403 | 33.8482 | 47.3237 | 61.9686 | 76.4911 | 94.5961 | 120.9792
270 | -37.9072 | -30.7107 | -26.485 | -26.1525 | -22.7983 | -19.5902 | -16.7218 | -12.6587 | -8.4055 | -3.714 | 0.91925 | 5.8429 | 11.9485 | 18.1949 | 24.2968 | 31.928 | 41.1012 | 56.8093
315 | 57.5145 | 49.0667 | 41.1341 | 30.7314 | 22.4626 | 12.2993 | 3.4459 | -3.6518 | -10.3804 | -16.0824 | -20.1163 | -24.7531 | -26.7152 | -29.3771 | -30.4733 | -30.6542 | -29.9362 | -27.4917
up | -255.4989 | -208.0584 | -173.6935 | -142.0598 | -114.8492 | -86.5113 | -58.5973 | -33.0365 | -6.1145 | 18.774 | 43.2552 | 68.0049 | 92.1352 | 117.7948 | 143.9129 | 171.7812 | 205.0883 | 247.7512
down | 182.6936 | 156.1406 | 135.9144 | 113.5837 | 94.0883 | 71.7665 | 48.7652 | 27.1104 | 5.4884 | -16.0952 | -35.7568 | -57.0444 | -75.6355 | -94.4623 | -113.8919 | -132.1961 | -154.0684 | -177.4497
degauss
measure
Pipe #1
11
Notes: Pipe degaussed in stated direction but measured

## Slide 12
Results - Pressurization
Chart: Radial Magnetic Field (uT)
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 105 | 110 | 115
degauss | -7.6475 | -15.137 | -28.3055 | -33.7265 | -30.152 | -25.369 | -21.5145 | -17.803 | -14.6075 | -11.591 | -8.1345 | -5.3695 | -1.932 | 1.4825 | 4.8575 | 8.4805 | 12.2825 | 15.606 | 18.949 | 22.2345 | 25.6345 | 25.9095 | 16.1555 | 7.841
1000 | -7.3725 | -14.919 | -27.4715 | -32.3435 | -28.873 | -24.432 | -20.6155 | -17.244 | -13.9825 | -10.615 | -7.3195 | -4.4605 | -1.524 | 1.8045 | 4.9525 | 8.5365 | 11.8185 | 14.753 | 17.736 | 20.2655 | 23.0215 | 22.2535 | 12.3675 | 6.089
2000 | -6.1415 | -12.855 | -26.4115 | -33.1205 | -28.551 | -23.958 | -20.7105 | -17.718 | -14.8065 | -10.606 | -7.9255 | -5.4445 | -2.5 | 0.3935 | 3.3145 | 6.2545 | 8.7975 | 11.42 | 13.144 | 14.3275 | 14.8965 | 16.8845 | 12.4145 | 6.24
3000 | -6.4155 | -12.741 | -24.9525 | -30.4215 | -26.373 | -22.387 | -19.4605 | -17.149 | -13.5935 | -10.587 | -8.1625 | -5.4355 | -2.178 | 0.8095 | 3.8545 | 7.0785 | 9.6785 | 12.149 | 14.081 | 15.4825 | 15.9945 | 18.8545 | 11.5055 | 5.653
0B | -8.4045 | -15.194 | -27.9835 | -34.8245 | -30.758 | -25.114 | -20.9845 | -17.093 | -13.8025 | -9.621 | -6.2975 | -3.0965 | -0.076 | 2.9595 | 5.9655 | 9.3035 | 12.7655 | 15.369 | 17.736 | 20.1895 | 21.8655 | 21.8185 | 13.5135 | 6.543
3000B | -6.6625 | -14.105 | -27.0175 | -31.2835 | -26.903 | -22.898 | -19.5165 | -16.969 | -13.7925 | -10.738 | -7.7745 | -4.9905 | -2.045 | 1.1415 | 4.4035 | 6.9465 | 9.9625 | 12.528 | 14.517 | 15.9375 | 17.2065 | 18.9395 | 11.6095 | 5.89
0C | -8.0255 | -15.933 | -30.3035 | -36.5485 | -32.282 | -26.08 | -21.4205 | -17.5 | -14.0295 | -9.687 | -6.2875 | -3.2105 | 0.047 | 3.1865 | 6.5245 | 9.8245 | 12.7935 | 16.07 | 18.447 | 20.4825 | 22.0555 | 21.9695 | 13.7405 | 6.562
Chart: Delta Radial Magnetic Field (uT)
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 105 | 110 | 115
1000 | 0.275 | 0.218 | 0.834 | 1.383 | 1.279 | 0.937 | 0.899 | 0.559 | 0.625 | 0.976 | 0.815 | 0.909 | 0.408 | 0.322 | 0.095 | 0.056 | -0.464 | -0.853 | -1.213 | -1.969 | -2.613 | -3.656 | -3.788 | -1.752
2000 | 1.506 | 2.282 | 1.894 | 0.606 | 1.601 | 1.411 | 0.804 | 0.085 | -0.199 | 0.985 | 0.209 | -0.075 | -0.568 | -1.089 | -1.543 | -2.226 | -3.485 | -4.186 | -5.805 | -7.907 | -10.738 | -9.025 | -3.741 | -1.601
3000 | 1.232 | 2.396 | 3.353 | 3.305 | 3.779 | 2.982 | 2.054 | 0.654 | 1.014 | 1.004 | -0.028 | -0.066 | -0.246 | -0.673 | -1.003 | -1.402 | -2.604 | -3.457 | -4.868 | -6.752 | -9.64 | -7.055 | -4.65 | -2.188
0B | -0.757 | -0.057 | 0.322 | -1.098 | -0.606 | 0.255 | 0.53 | 0.71 | 0.805 | 1.97 | 1.837 | 2.273 | 1.856 | 1.477 | 1.108 | 0.823 | 0.483 | -0.237 | -1.213 | -2.045 | -3.769 | -4.091 | -2.642 | -1.298
3000B | 0.985 | 1.032 | 1.288 | 2.443 | 3.249 | 2.471 | 1.998 | 0.834 | 0.815 | 0.853 | 0.36 | 0.379 | -0.113 | -0.341 | -0.454 | -1.534 | -2.32 | -3.078 | -4.432 | -6.297 | -8.428 | -6.97 | -4.546 | -1.951
0C | -0.378 | -0.796 | -1.998 | -2.822 | -2.13 | -0.711 | 0.094 | 0.303 | 0.578 | 1.904 | 1.847 | 2.159 | 1.979 | 1.704 | 1.667 | 1.344 | 0.511 | 0.464 | -0.502 | -1.752 | -3.579 | -3.94 | -2.415 | -1.279
Pipe #3
Degaussed in situ
12

## Slide 13
Results - Pressurization
Chart: Radial MAgnetic Field (uT)
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 105 | 110 | 115
degaussed | 1.7375 | 3.101 | 4.6305 | 5.5355 | 6.629 | 7.007 | 6.2885 | 4.896 | 3.1395 | 1.43 | -0.0185 | -1.8845 | -3.523 | -5.1845 | -6.7335 | -7.8835 | -9.6115 | -11.137 | -12.936 | -14.2145 | -15.3695 | -14.0245 | -8.7695 | -5.445
1000 | -0.2135 | -0.649 | -2.1595 | -2.4105 | -0.919 | 0.028 | 0.3795 | 0.133 | -0.3645 | -0.985 | -1.4955 | -2.7175 | -3.447 | -3.9535 | -4.6685 | -4.8915 | -5.7955 | -6.781 | -7.567 | -8.3425 | -8.6835 | -6.9695 | -4.6215 | -3.372
2000 | -1.6435 | -4.01 | -8.8545 | -10.8095 | -8.494 | -6.932 | -6.1075 | -5.833 | -4.9105 | -4.034 | -3.8345 | -4.1095 | -3.968 | -3.4985 | -2.9835 | -2.5425 | -2.1305 | -2.216 | -2.131 | -2.1875 | -2.0355 | 0.6915 | 0.0945 | -0.9
3000 | -3.1395 | -6.889 | -14.2335 | -17.1925 | -14.138 | -11.856 | -10.3785 | -9.763 | -7.8365 | -6.288 | -5.8045 | -5.2175 | -4.318 | -2.7695 | -1.6855 | -0.2505 | 1.0705 | 2.121 | 2.822 | 3.5135 | 4.0245 | 7.7465 | 4.4885 | 1.259
0B | -4.6735 | -8.622 | -16.3355 | -20.0045 | -17.472 | -13.684 | -11.3255 | -9.697 | -7.7035 | -5.587 | -4.1375 | -3.2765 | -2.112 | -0.9805 | 0.1605 | 1.4825 | 3.0585 | 4.128 | 5.549 | 6.7615 | 7.8125 | 9.1765 | 6.4585 | 1.808
3000B | -3.2435 | -7.495 | -14.5925 | -17.6085 | -14.706 | -12.349 | -10.9565 | -10.151 | -8.4425 | -6.932 | -6.1265 | -5.3975 | -4.185 | -2.9405 | -1.3825 | 0.1945 | 1.4775 | 2.935 | 3.816 | 4.4795 | 5.0385 | 9.0905 | 5.3125 | 1.467
0C | -5.1945 | -10.431 | -19.3655 | -22.1355 | -18.797 | -14.972 | -12.3485 | -10.132 | -7.8365 | -5.464 | -3.9585 | -2.9445 | -1.648 | -0.2035 | 1.2215 | 3.1395 | 5.0475 | 6.505 | 7.822 | 9.3745 | 11.0515 | 11.8185 | 5.6815 | 1.856
3000C | -3.6985 | -8.139 | -16.0515 | -18.8215 | -16.051 | -13.39 | -11.6005 | -10.53 | -8.8685 | -7.168 | -6.0605 | -5.2745 | -3.996 | -2.7415 | -0.8235 | 0.7335 | 2.1025 | 3.494 | 4.924 | 5.3315 | 6.4495 | 9.6595 | 5.5015 | 1.714
0D | -5.2985 | -10.848 | -18.8355 | -21.7565 | -18.343 | -14.792 | -12.3865 | -10.161 | -7.8455 | -5.729 | -3.8535 | -2.7275 | -1.42 | -0.0145 | 1.6945 | 3.4615 | 5.4825 | 6.723 | 8.447 | 9.7255 | 11.6005 | 11.8185 | 5.7285 | 2.017
Pipe #3
Degaussed in reverse direction
13

## Slide 14
Results – Pressure and Bending
Chart: Distance (cm)
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150
degauss | -238.4973 | -206.0524 | -183.5115 | -168.0245 | -155.6469 | -140.2931 | -129.7845 | -119.1663 | -110.5504 | -98.6258 | -94.4001 | -86.8786 | -80.7071 | -73.5802 | -67.1603 | -61.8621 | -59.0376 | -51.4284 | -48.5016 | -43.8978 | -28.1166 | -22.8111 | -18.7132 | -13.2488 | -8.0529 | -0.6666 | 3.1846 | 9.0053
2000 psi | -231.7321 | -197.8111 | -176.4577 | -161.1314 | -147.2976 | -133.7527 | -124.4681 | -114.8108 | -106.1127 | -95.3154 | -90.6731 | -83.6832 | -78.0818 | -69.5098 | -63.7658 | -60.5906 | -59.0157 | -50.82 | -47.2685 | -42.3521 | -28.1786 | -20.9239 | -17.0671 | -11.6648 | -5.9355 | -0.68115 | 1.4947 | 7.7776
bent | -186.0437 | -162.739 | -148.0851 | -135.0114 | -120.8489 | -112.264 | -102.7347 | -95.6608 | -82.3605 | -78.2937 | -70.5602 | -63.194 | -55.4313 | -54.6457 | -47.6448 | -47.6503 | -43.8265 | -40.5819 | -38.563 | -37.6277 | -34.0139 | -28.1896 | -22.3744 | -16.488 | -12.6751 | -10.1942 | -6.3027
unbent | -225.2116 | -190.4704 | -168.3807 | -152.3528 | -140.1433 | -125.2647 | -116.0276 | -105.508 | -98.7939 | -87.9145 | -84.9494 | -77.7311 | -71.7807 | -63.046 | -59.6114 | -56.2589 | -55.106 | -47.1022 | -45.0907 | -40.421 | -28.7743 | -24.8024 | -20.6772 | -17.6408 | -12.2111 | -8.802 | -7.0316 | -2.9521
0 psi | -234.5474 | -196.8391 | -172.4475 | -154.2182 | -139.6391 | -126.3755 | -116.0185 | -105.8332 | -98.3244 | -89.5148 | -86.1587 | -79.5215 | -73.5784 | -66.1719 | -60.2635 | -56.7083 | -53.4856 | -47.4931 | -45.3008 | -40.5471 | -24.9066 | -20.7868 | -17.1475 | -12.9766 | -9.2642 | -5.3198 | -4.3935 | 0.0167
Pipe #2
Degaussed in situ
4 point bend – Max stress 200 MPa
0
150
14
Stress
200 MPa
Notes: Stress is approximately constant between 100 and 150 cm. Tapers to 0 at 0 cm (end of pipe)

## Slide 15
Results – Pressure and Bending
Chart: Distance (cm)
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95 | 100 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150
degauss | 89.1262 | 81.9865 | 76.3066 | 71.4103 | 66.4958 | 63.0593 | 57.8196 | 56.464 | 50.2615 | 49.5855 | 46.1582 | 43.869 | 39.793 | 39.2888 | 35.8944 | 34.6849 | 32.1071 | 30.7953 | 33.0425 | 33.5249 | 32.8726 | 30.1504 | 23.6063 | 20.5224 | 15.8874 | 10.1837 | 5.4171 | 2.6676
2000 psi | 32.699 | 35.2092 | 42.2741 | 44.3276 | 46.0541 | 46.0011 | 43.3903 | 47.1046 | 40.8563 | 42.0712 | 38.496 | 34.632 | 34.2409 | 33.5759 | 33.3896 | 30.4793 | 27.5086 | 26.4764 | 29.6517 | 30.2144 | 36.5996 | 34.3908 | 27.326 | 27.5287 | 20.9774 | 16.1633 | 11.7457 | 7.2734
bent | 20.6028 | 20.2082 | 22.2927 | 23.7268 | 20.9609 | 18.6936 | 19.6272 | 13.8302 | 15.1749 | 13.1562 | 8.9395 | 9.8402 | 15.6901 | 11.7037 | 10.5235 | 9.0199 | 9.4146 | 9.7561 | 12.7688 | 12.2792 | 9.8037 | 5.8483 | 8.8262 | 5.6163 | 2.4922 | 1.5605 | -1.1854
unbent | 6.4695 | 10.6367 | 13.3644 | 16.578 | 17.4367 | 14.9393 | 12.197 | 15.6097 | 8.7149 | 9.8311 | 8.1174 | 4.1968 | 4.7741 | 7.4122 | 8.0406 | 8.0243 | 6.5882 | 5.9909 | 11.1063 | 14.6104 | 23.0472 | 20.5078 | 16.5854 | 18.4488 | 14.4295 | 9.8804 | 6.6723 | 3.7674
0 psi | 5.2564 | 12.8291 | 15.849 | 19.6437 | 21.8195 | 19.2709 | 18.2844 | 20.2521 | 13.4612 | 13.5563 | 12.1513 | 8.1174 | 7.9256 | 9.2556 | 9.8091 | 8.4517 | 8.9943 | 8.7916 | 11.6508 | 15.7449 | 21.9182 | 21.8122 | 18.9366 | 19.1193 | 15.1274 | 11.7914 | 8.2562 | 4.3045
15
Notes: Although stress at 0 is 0 that is where the biggest change in magnitude occurs

## Slide 16
Summary
Earth’s field is too weak to act on its own but can produce effects in conjunction with stress and external magnetic fields
The effect of stress depends on the magnetic state of the object being stressed.
16

## Slide 17
Summary
Magnetic samples are linked magnetic objects, i.e. an effect can propagate a long way from the impetus
It is very difficult to achieve a reproducible magnetic ground state
17

## Slide 18
Outstanding Questions
Why do pipes behave like non-uniform weak magnets?
18

## Slide 19
Future Work/Applications
Develop a macroscopic model for large magnetic samples based on microscopic dipoles & pinning
Can we use an induced magnetic state to measure stress history?
19

## Slide 20
Questions?
20