## Slide 1: Static elastic modulus prediction at early ages using a modified test for concrete cylinders using MEMS microphones
Cristobal A. Lara, Giovanni Cascante, José F. De la Mora.

## Slide 2
Introduction
Test Methodology
Forecasting Methodology
Conclusions
OUTLINE
p.2

## Slide 3
Introduction – Static Test
Standard Concrete Cylinders
10x20 cm
Quality Assurance
Standard for static test
Construction Site
Compressive Strength (fc)
Young’s modulus (E)
p.3

## Slide 4
Introduction – Static Test
Main Drawbacks
Transportation of specimens required
Time consuming
Modulus of elasticity is often disregarded from the test
Expensive test equipment required
Non-repeatable (destroy the specimens)
Main Advantage
Good representation of real loading conditions
[1]
p.4

## Slide 5
Introduction – Dynamic Test
Main advantages
Non-destructive allowing repeatable testing (maturing monitoring)
More portable & affordable equipment
Faster Testing
Main Drawback
Test does not represent real loading cases
[2]
p.5

## Slide 6
Strain levels difference
  Static: 1E-3 [1]
  Dynamic: ~6E-6 [3]
Ed > ES
Poisson’s ratio
  Static: 0.15 - 0.20
  Dynamic: 0.20 - 0.30[4]
Introduction – Static & Dynamic differences
Chart: Strain
| 0 | 5.2500000000000002E-5 | 9.2499999999999999E-5 | 1.45E-4 | 2.0250000000000002E-4 | 2.6499999999999999E-4 | 3.2250000000000003E-4 | 3.8249999999999997E-4 | 4.4499999999999997E-4 | 5.0999999999999993E-4 | 5.7249999999999998E-4 | 6.3750000000000005E-4 | 7.074999999999999E-4 | 7.7749999999999998E-4 | 8.5250000000000007E-4 | 9.2749999999999994E-4 | 1.0075000000000001E-3 | 1.0924999999999999E-3 | 1.1849999999999999E-3 | 1.2850000000000001E-3 | 1.3850000000000002E-3 | 1.4974999999999999E-3 | 1.6250000000000001E-3 | 1.7625E-3 | 1.92E-3 | 2.0975E-3 | 2.3275000000000001E-3
Test readings | 0 | 0.55494 | 1.1099 | 1.6648 | 2.2198 | 2.7747 | 3.3297 | 3.8846 | 4.4395 | 4.9945 | 5.5494 | 6.1044 | 6.6593 | 7.2143 | 7.7692 | 8.3241 | 8.8791 | 9.434 | 9.989 | 10.5439 | 11.0989 | 11.6538 | 12.2087 | 12.7637 | 13.3186 | 13.8736 | 14.0956
 | 0.52852 | 5.6382
 | 5.6382
 | 14.0956
Dynamic Strain
Range
p.6

## Slide 7
Introduction – Research Goal
Develop a simpler, more affordable and faster test methodology
Proposed a forecasting methodology to estimate the elastic static modulus at early ages
[2]
[5]
p.7

## Slide 8
Methodology - Outline
Validate test methodology
Proposed testing methodology
  Impact and sensor locations
  Impact hammer
  Cylinder support
  Signal processing
  Dynamic elastic modulus
Forecasting methodology
…
p.8

## Slide 9
Proposed Testing Methodology
Cylinder over foam
Impact at top surface near and edge
Microphone placed opposite end
Hammer with diameter tip around L/10
Record audio signal with multiple impacts
⌀≈L/10
p.9

## Slide 10
D, L and νD dependant
Proposed Testing Methodology
p.10

## Slide 11
Outline
Impact & sensor location
Hammer selection
Support method
Signal processing
Proposed Testing Methodology
p.11

## Slide 12
Methodology – Microphone and Impact Location
The objective is to excite and capture both fundamental modes, longitudinal and flexural
Finite Element Analysis
6.00 kHz
10.94 kHz
9.55 kHz
Sensor
p.12
Cylinders average dimensions:
D: 10.2 cm L: 20.1 cm ρ: 2.3 g/cm3

## Slide 13
Methodology – Hammer Selection
The maximum excitation frequency can be estimated by Hertz theory
p.13
[6]
[7]
The time of contact tc can be approximated as a function of the impact sphere diameter:

## Slide 14
Free falling sphere test using different support conditions
Methodology – Support Selection
p.14

## Slide 15
Testing different hammer handles
Methodology – Hammer Selection
Support: Foam
H | Sphere Diameter (ds) |  | fmax [kHz]
 | [in] | [mm] | 
06 | 1/4 | 6.4 | 54.9
07 | 7/16 | 11.1 | 31.4
08 | 1/2 | 12.7 | 27.5
09 | 3/4 | 19.1 | 18.3
10 | 1/2 | 12.7 | 27.5
11 | 3/4 | 19.1 | 18.3
p.15

## Slide 16
Recap:
A single test requires several (≳10) impact recordings in a single audio file
Methodology – Signal processing
p.16

## Slide 17
Methodology – Signal processing
p.17
The filter algorithm uses the ratio between flexural and longitudinal vibration frequencies
[8]
[9]

## Slide 18
Methodology – Signal processing
p.18
The filter algorithm uses the ratio between flexural and longitudinal vibration frequencies
A Monte Carlo simulation is used to estimate the 99% confidence interval for the frequency ratio.
The mean and standard deviation for L, D, and ν are used

## Slide 19
Methodology – Signal processing
p.19
A quality index is defined to qualify the peaks in the amplitude spectra
QR: Ratio index
QP: Prominence index
QM: Magnitude index
QR
QP

## Slide 20
Methodology – Signal processing
p.20
This algorithm separate the potential impacts (shown in red, black and blue)
Detect Individual Impacts

## Slide 21
Methodology – Signal processing
p.21
Frequency Selection Algorithm

## Slide 22
Methodology – Signal processing
p.22

## Slide 23
Methodology – Dynamic elastic modulus
p.23
Once the longitudinal resonant frequency is found. The dynamic elastic modulus can be computed

## Slide 24
Outline
Forecasting Methodology Overview
  Dynamic elastic modulus vs age relationship
  Static-dynamic elastic modulus relationship
  Estimation of static modulus at 28th day
Forecasting Methodology
p.24

## Slide 25
p.25
Proposed Forecasting Methodology
Test cylinders dynamically with time and compute linear regression
Correlate the dynamic modulus regression to static modulus using their relationship
Estimate the expected static value based on the extrapolation of the linear regression

## Slide 26
p.26
Forecasting Methodology
Young’s modulus vs Age
Both, static and dynamic elastic modulus mature linearly in semi logarithmic plot (between 1-28th day)

## Slide 27
p.27
Forecasting Methodology
Static vs Dynamic elastic modulus
The relationship between both moduli is linear

## Slide 28
p.28
Forecasting Methodology
Estimation of Static modulus at 28th day
The relationship between both moduli is linear

## Slide 29
Conclusions
When using the test setup and the signal processing algorithm proposed, the resonant frequencies were accurately found for all tests
Based on the linearity of the elastic moduli and age, it’s possible to accurately forecast the static modulus using early age measurements of the dynamic modulus.
The 95% confidence interval for the static modulus found was within ±7.4% of the expected value.
However the actual error for the estimation for the computed example was less than 2%
Methodology useful for cylinders with length between 11 – 50 cm. (Assuming an L/D =2)
p.29

## Slide 30
Special considerations
Methodology useful for cylinders with length between 11 – 50 cm. (Assuming an L/D =2)
Smartphones microphones required validation of relatively flat frequency response within band of interest
It is recommender to use a hammer with low mass handle.
For concrete, it is recommended a steel sphere with diameter around 10% the length of the cylinder.
The impact and microphone location have large tolerancies
The foam support could be optional. But it is recommended for cleaner signals
The ES-ED relationship is recommended to be obtained by the concrete supplier
p.30

## Slide 31
[1] ASTM C39/C39M, Standard test method for compressive strength of cylindrical concrete specimens. 2018, ASTM International: West Conshohocken.
[2] Boone, S.D., A comparison between the compressive strength and the dynamic properties of concrete as a function of time. 2005, University of Tennessee, Knoxville.
[3] Bay, J.A. and H. Stokoe, Field and laboratory determination of elastic properties of portland cement concrete using seismic techniques. Transportation Research Record, 1992(1355).
[4] Neville, A.M., Properties of concrete. 1996: Pearson.
[5] Free Icon Library. 2019; Available from: https://icon-library.net/.
[6] Carino, N.J. The impact-echo method: an overview. in 2001 Structures Congress & Exposition. American Society of Civil Engineering.
[7] Lin, Y., M. Sansalone, and N. Carino, Impact-echo response of concrete shafts. Geotechnical Testing Journal, 1991. 14(2): p. 121–137-121–137.
[8] Love, A.E.H., A Treatise on the Mathematical Theory of Elasticity. 1944: Cambridge University Press Warehouse.
[9] ASTM C215/C215M, Standard test method for fundamental transverse, longitudinal, and torsional resonant frequencies of concrete specimens. 2014.
References
p.31

## Slide 32
References
p.32
The Natural Science and Engineering Research Council of Canada (NSERC), the Ontario Centres of Excellence, the Ministry of Transportation of Ontario, (MTO), for their financial support; and to Mr. Ed Ginzel his strong technical and personal support to our research group.