## Slide 1: Evaluation of progressive damage in GFRP bars – low and large strain experimental programme and numerical simulations
Piotr Wiciak, Ph.D, Kinectrics Inc., formerly at University of Waterloo
Contact: pwiciak@uwaterloo.ca
Maria Anna Polak, Ph.D, Professor, University of Waterloo
Giovanni Cascante, Ph.D, Professor,University of Waterloo

## Slide 2: Outline
Introduction
Methodology
Results
  Numerical simulation
  Ultrasonic evaluation
  Shear test
  Results comparison
Study of GFRP/concrete compromised bond
Conclusions

## Slide 3: Introduction
What are we trying to solve?
Long-term durability of GFRP in concrete – unresolved issue.
Current solutions: tensile, flexure, and shear tests – destructive, high-capacity test frames required, lab required => nondestructive testing (NDT) methods
Available NDT (corrosion of steel rebars):
  visual inspection
  electromechanical
  electromagnetic (ground-penetrating radar, magnetic flux leakage, or passive magnetic inspection)
  elastic wave methods (passive methods [acoustic emission] and active techniques: impact, echo, ultrasonic pulse velocity, and ultrasonic guided wave).
The GFRP bars are nonmagnetic => no or decreased applicability of the magnetic methods.
Notes: the long-term durability of GFRP in concrete remains an unresolved issue. It is also the main reason why the widespread application of GFRP cannot be readily accepted
Current solutions: tensile, flexure, and shear tests – destructive, high-capacity test frames required, lab required => nondestructive testing (NDT) methods
Available NDT (corrosion of steel rebars):
  visual inspection
  electromechanical (such as half-cell potential, galvanostatic pulse polarization, and electrochemical impedance spectroscopy[15]-[18]),
  electromagnetic (e.g. ground-penetrating radar, magnetic flux leakage, stress-induced magnetic anisotropy, or passive magnetic inspection [16], [19]-[21]) and
  elastic wave methods (including passive methods such as acoustic emission (AE [22]) and active techniques: impact, echo, ultrasonic pulse velocity, and ultrasonic guided wave [23]-[26]).
The GFRP bars are nonmagnetic, which results in no or decreased applicability of the magnetic methods.

## Slide 4: Introduction
Challenges
Composite materials => anisotropy.
Fibre scattering + high attenuation of epoxy resins => frequency range (1-10 MHz)
GFRP bars: have unidirectional fibres composition
Internal reinforcement in concrete => properties in the longitudinal direction
The gap
Amplitude-based techniques were not applied to GFRP bars
Shear test vs ultrasonic testing (UT) for GFRP bars at different deterioration levels = ?
Bar diameter and frequency effects on the ultrasonic features (below 150 kHz) = ?

## Slide 5: Methodology
Five activities:
GFRP bars conditioning (i.e. accelerated ageing test in alkaline solution)
ultrasonic evaluation
reference intrusive test (i.e. shear test)
numerical modelling of wave propagation in GFRP bars and damage progression
Application: detection of concrete/GFRP rebar bond loss
SPECIMENS
336 bars per diameter (D13, D16, D20, and D25) are used.
The alkaline immersion (pH of 12.6-13 @ 60°C).
Equivalent of the environment that bars would experience in concrete
Bars are kept in the solution for up to 6 months. Every month (i.e. 28 days),
Set of 12 short specimens (per D) is obtained per diameter. Six specimens => shear test, and the remaining six bars => Ultrasonic Test
Pilot study of damage evaluation in bare GFRP bars.
Prerequisite step before evaluating bars embedded in concrete member.

## Slide 6: Background
Wave propagation in a solid cylinder
(Pochhammer-Chree theory: infinite homogeneous, isotropic cylinder of uniform cross-section)
Alkaline ingress model: Katsuki and Uomoto
Failure strength can be estimated with the unaffected cross-sectional area of the GFRP bar:
– penetration depth measured for the surface of the rod
– mass diffusion coefficient
c – alkaline concentration
t – time

## Slide 7: Ultrasonic (UT) Evaluations Setup
± 125V
Notes: Characterization
Laser vibrometer: flat bandwidth 30 kHz – 24 MHz
A function generator provides 150 kHz square pulses (±5V) to UTx.
UT
axial setup: UT transducers on both ends of a bar.
3-D printed caps (printed out of PC-ABS) => concentric position,
3-D printed holders (PC-ABS, with elastic bands) => equal coupling
Laser scanning
Similar to axial setup 75 to 171pts rec.

## Slide 8: Results – UT evaluation
UT characterization and why it’s important

## Slide 9: Results – UT evaluation
UT Evaluation
Ultrasonic evaluation trends: (a) wave velocity trend-axial configuration, (b) wave velocity-transverse configuration, and (c) P-Peak attenuation trend-axial configuration
Axial - AMPLITUDE
Notes: The normalized wave velocity trends (in the axial configuration) show a consistent decrease with the progression of damage. However, the velocity reduction is within 5%, which does not offer enough sensitivity for field applications. No consistent conclusion can be made regarding the effect of bar diameter on the wave velocity.
In the transverse configuration, a diameter effect is observed on the reduction rate (besides 13mm bar). The largest diameter is affected the least. This behaviour is expected, as the depth of penetration is the same for all bar diameter, which affects the smallest bars the most. At the same time, velocity reduction in the transverse configuration is low and reaches 2% after six months of conditioning.
Wave amplitude change with induced damage shows that P-Peak amplitude is a more sensitive parameter (a reduction of up to 40% is observed), capable of capturing the deterioration of the GFRP bars. The amplitude-based approach for field applications requires more laboratory tests with GFRP bars embedded in concrete (with different levels of deterioration in the bars). A possible solution for the issue of coupling is to use spring-loaded sensors or load cells.

## Slide 10: Results – numerical model
Assumptions and model details
Numerical model developed by the authors is used to explore the wave propagation in GFRP bars.
The following assumptions are made:
  the bar is assumed to have a perfect circular cross-section
  the deterioration follows the model proposed by Katsuki and Uomoto
  the affected outer radial section of the bar has significantly reduced stiffness and can be removed from the model.
The numerical simulation is meant to supplement lab experiments.
Both axial and transversal vibrations are simulated.
Material damping is simulated with a Rayleigh damping model available in Abaqus
https://doi.org/10.1016/j.mtcomm.2021.102199
Notes: GFRP is simulated as a linear elastic material (the wavelength is significantly larger than fibre size).

## Slide 11: Results – numerical model
Real excitation
Excitation - frequency
Calibration results

## Slide 12: Results – numerical model
Numerical results follow the theoretical dispersion curves.
Relative difference for the most sensitive frequency range (D13: 180-380 kHz, and D25: 90-190 kHz
wave dispersion can be recommended for the monitoring of the GFRP bar condition. The benefit is that it considers the whole array of data points, which should minimize the testing errors.
Theory
Model

## Slide 13: Results – Shear test
Shear test details: (a) photograph of the shear device, (b) schematic highlighting the most important parts, and (c) example of stress-displacement curves calculated for unconditioned D13 bars
Decreasing trends are observed for all bar diameters, and the dependency with bar diameter can be distinguished (i.e. larger bars are affected less).
Notes: shear strength is normalized with respect to the baseline condition. The shear strength change with the damage plot for all of the bars is shown in Fig. 12b. The obtained trends follow the findings of Arczewska [14]. Decreasing trends are observed for all bar diameters, and the dependency with bar diameter can be distinguished (i.e. larger bars are affected less). The depth of penetration of the alkaline solution is the same for all of the bar diameters (Equation 1); therefore, the cross-sectional area of larger bars is reduced less, which results in a lower reduction of shear strength.

## Slide 14: Results – Results comparison
Curve fitted test results (lines represent fitted lines, and symbol markers are used for data points: (a) P-Peak amplitudes from ultrasonic evaluation, (b) shear strength change, and (c) dispersion change from numerical simulations. The box in figure (a) shows data points that are excluded from the fitting procedure
, x is the bar condition, and a and b are the coefficients of the fitted line) is fitted to the analyzed features

## Slide 15: Results – Results comparison
Comparison between normalized degradation fitted curves for (a) ultrasonic evaluation and shear strength data, and (b) numerical simulation and shear strength.
Notes: The comparison of the large strain (shear strength retention) and low strain (corrected ultrasonic attenuation fitted curves) properties show some differences, but decreasing trends are the same for both features. It demonstrates that low strain measurements can be used to estimate the effect of progressive damage on large strain properties in GFRP bars. The maximum relative error (calculated as a difference between the two methods normalized with the shear test) between the two test methods is 6.77% (D13). When the shear test data and corrected numerical simulation are considered, an improved correlation between the tests is observed. The maximum relative error between the two curves is 1.85%.

## Slide 16: Study of GFRP/concrete compromised bond
UT: axial configuration.
P-wave ultrasonic transducers (54 kHz and 150 kHz).
Ultrasonic transducers are placed on both ends of each bar
3-D printed caps are used
16 time-averages
Debonded areas => wrapping three layers of plastic wrap around the bars (i.e. 0, 20, 40, 60, 80, and 100 % of length).
Six D20 are embedded in three concrete beams
Bond loss: (i.e. 0, 20, 40, 60, 80, and 100 %).
Industrial concrete batch (30 MPa); coarse aggregate: 19mm
At the age of 28 days, the average compressive strength is 34.86±1.67 MPa.

## Slide 17: Study of GFRP/concrete compromised bond
Bond quality does not affect the arriving wave significantly (up to 7%)
The PP amplitudes reported for fully debonded bars are 17-19 X HIGHER than for the perfect bond
The amplitude approach is extremely sensitive for the identification of bond loss between concrete and GFRP bars.
Possible solution includes the use of non-structural bars that allow for bar ends access.
The next: measure energy at the concrete.
Notes: Bond quality does not affect the arriving wave significantly (up to 7%) change is observed in the recorded signals. The change is associated mostly with a difficulty of the selection of the true first arrival time, which is affected by different amplitude levels of the propagating waves. Next, peak-to-peak (PP) amplitudes are extracted from the signals recorded with 54 and 150 kHz transducers. Fig. 14d presents a distribution of PP values for both transducers with the progression of bond loss between concrete and GFRP. An increase of the PP amplitude with the progression of the bond loss is observed. The PP amplitudes reported for fully debonded bars are 17-19 times higher than for the case of the perfect bond between the two materials (an almost exponential amplitude growth with damage is observed). This application shows that the amplitude approach is extremely sensitive for the identification of bond loss between concrete and GFRP bars. However, the true challenge is related to the field application. Again, the possible solution includes the use of non-structural bars that allow for bar ends access. These diagnostics bars can be used for the periodical analysis of reinforcement bond quality. The next steps of this bond quality study include analysis of energy measured at the concrete cover on top of the bars. It is anticipated that the measured signal for the well-bonded bars should have higher amplitudes than for the bars with compromised GFRP/concrete bond

## Slide 18: Conclusions
Wave amplitude approach
  superior to wave velocity (reduction of up to 40% is observed)
  laboratory tests with GFRP bars embedded in concrete (field applications )
Dispersion curves: different frequency ranges offer increased sensitivity. Select ultrasonic transducers based on tested bar diameter
Numerical model (dispersion curves @ low strains) shows good agreement with shear test findings in the literature (large strains).
The shear test results obtained in this study show good agreement with the data reported in the literature.
The application of the wave amplitude approach for the evaluation of bond loss between GFRP bars and concrete shows the extreme sensitivity of that elastic feature for the change in bond quality.

## Slide 19: Conclusions
Ultrasonic evaluation (low-strain measurement) can capture the declining condition of the GFRP bar and, with proper analysis (the correction factor), can be used to obtain an estimate of the shear strength (and consequently tensile strength) reduction (large-strain measurement). The maximum error of the ultrasonic evaluation with respect to the shear test is less than 7%.

## Slide 20: Acknowledgements
The Natural Science and Engineering Research Council of Canada (NSERC), the Ontario Centres of Excellence, the Ministry of Transportation of Ontario, (MTO), for their financial support; and to Mr. Ed Ginzel his strong support to our research group.