## Slide 1: NDE 4.0 in Body-in-White Vehicle Assembly Process
R. Gr. Maev*, A.M. Chertov*, D. Stocco*, M. Rodzik**, J. Chamberlain**
*Institute for Diagnostic Imaging Research, Windsor, ON
** The Narmco Group

## Slide 2
Resistance Spot Welding in Industry
Regular vehicle contains 4000-6000 spot welds
Spot welding is highly automated today.
So it has to be inspected regularly.

## Slide 3
“Without question, the dominant joining technology in automotive construction today is resistance spot welding. A typical body-in-white constructed today contains as many as 6000 resistance spot welds. A recent automotive roadmap suggests that trend is not likely to change any time soon.”
Gould, J. E. (Edison Welding Institute)
Welding Research
01 2012, V. 91 pp. 23-s to 34-s
What is the Future of Spot Welding?

## Slide 4
Spot Welding
4
Spot welding involves
electrode forces: 500..2200 lb
electric currents: 5000..13000 A
temperatures: 20..2000 C
Outside (top) and inside (bottom) look of spot weld
Some means of quality control are required to ensure uninterrupted automatic production.

## Slide 5
5
5
Peel test Cross-section
Cons: Selective testing; Time consuming; Labour intensive.
More than 99% of the parts are never checked. For this reason, at the design stage, additional spot welds are introduced into the assembly process.
Destructive Testing

## Slide 6
Testing Configuration
6
Ultrasonic wave is sent by the ultrasonic transducer positioned in the cooling water stream. Reflections from the stack boundaries and nugget tell whether the base metal is melted or not.

## Slide 7
7
Non-destructive Testing
When steel plates are heated, the sound speed drops from 5900 m/s at room temp. down to 4200 m/s at melting point and down to 3900 m/s in liquid state.
Potential to inspect 100% of produced welds
steel
steel

## Slide 10
Calculate parameters from coordinates obtained by Deep Learning and match them with real weld geometry
Matching Weld Geometry with Ultrasonic Measurements using AI

## Slide 11
The Hardware

## Slide 12
Every horizontal row of tags represents welds on one part.
RIWA can get Weld ID and Part ID from the robot and break the welds into parts or logical groups of welds.
Production Data Example

## Slide 13
Welding Cell with Multiple Robots

## Slide 14
Welding Cell with Multiple Robots and Networked Ultrasonic Testers

## Slide 20
Plant-wide Aggregation of the Assembly Process Quality Data

## Slide 21
Quality Status Displayed in Real Time
Example of Graphical Representation of Weld Monitoring in Production
Trends in weld quality can easily be spotted

## Slide 22
Automated Inspection of 100% of Welds vs Manual Inspection

## Slide 23
Conclusions
AI-driven automation of quality inspection reduces costs on scrap, maintenance and manual selective inspections
Real-time quality characterization and process monitoring
Operator-independent
Data analysis allows determine trends and predict certain failure modes
Quality data can be saved for long-term potential use (life of the product)