## Slide 1: Separating Microstructural and Stress Effects on MBN Energy Parameter in Temper Embrittled Steel
Mehrdad Kashefi a, Thomas W. Krausea, P. Ross Underhilla, Aroba Saleema and Shannon P. Farrellb
aDepartment of Physics and Space Science, Royal Military College of Canada, Kingston, ON, K7K 7B4, Canada
bDefence Research and Development Canada, Atlantic Research Centre, Dartmouth, NS, Canada

## Slide 2
Introduction
  Non-destructive MBN technique
  Effect of Stress
  Temper embrittlement
Material & Methods
  MBN set up
  Sample preparation
Results & Discussion
Conclusion
  2

## Slide 3
Ferromagnetic materials are made of micron-size magnetic regions called domains
Domains are separated by domain walls (DWs)
  180 o and 90 o DWs
Domains that are most closely aligned with the applied field grow at the expense of other domains
Under external magnetic field domain walls movement happen
  Change in domain structure in the material
    Magnetization
3
Introduction
  3

## Slide 4
Irregularities in microstructure act as pinning sites for domain wall motion
Grain boundaries, Inclusions, Dislocations and Precipitants (carbides, oxides)
The presence of these pinning sites during magnetization results in abrupt domain wall motion
MBN signals are mainly generated by the movement of 180° domain walls
      discontinuous magnetization happens
        Magnetic Barkhausen Noise (MBN)
4
  4

## Slide 5
MBN Analysis
Evaluating MBN emissions
MBN energy: Integral of the voltage squared signals over time
(The area under squared voltage)
  5

## Slide 6
MBN Response to Stress
(active or residual stress)
Below the yield strength
(elastic zone)
uniaxial tensile stress along the RD MBN energy
the increase of the active 180 domain wall population and reduction of the 90 domain volume
  6
  Quality control tool
    residual stress evaluation
    microstructural characterization
    mechanical properties evaluation
      bulk and case heat treatment, grinding, welding, casting
Notes: Sensitivity to both stress and microstructure
  Quality control tool
    residual stress evaluation
    microstructural characterization
    bulk and case heat treatment, grinding, welding, casting
    mechanical properties prediction, such as hardness and

## Slide 7
Temper Embrittlement (TE): Reduction in toughness as a result of exposure in the temperature range between 400-600 °C
    increase in likelihood of fracture
Mechanism: Carbide formation and/or segregation of impurities ( P, S, Sn, Sb) to prior austenite grain boundaries.
    an intergranular crack path
Traditional technique for TE detection:
    Impact toughness test
  7
Notes: In Practice:
post-fabrication heat treatments (residual stress relief)
long term high temperature service application

## Slide 8
Parameter | Mechanism | MBN energy
Tensile stress | Increases 180° domain wall population, which results in more interaction with pinning sites | Increase
Pinning site density | Less pinning sites decrease interaction with 180° domain walls | Decrease
Combined effects of tensile stress and temper embrittlement on MBN energy
  8

## Slide 9
Material and methods
Sample | Q1 | Q2 | Q3 | Q4 | Q5
Heat treatment time (hr) at 525°C | 0 hr | 48 hrs | 96 hrs | 168 hrs | 336 hrs
Heat treatment regime
% | C | Si | Mn | Cr | Ni | Mo | Cu | P | S
Q1N | 0.16 | 0.25 | 0.31 | 1.42 | 2.71 | 0.41 | 0.1 | 0.01 | 0.008
In-house MBN flux control testing device with a
tetra-pole probe
Flux sweep from 0.1 T to 1 T (in 0.1 T steps)
Rolling (RD) and transverse (TD) directions (same location)
Frequency: 50 Hz
Tetra-pole Probe
Pick-Up
Coil
Magnetization
core
9
  9
Q1N Steel: (low carbon-low alloy)- Susceptible to TE
Notes: The U-core electromagnet magnetizes the sample
Pick- up coil senses resulting BN emissionsNoise
Destructive, time consuming, and expensive

## Slide 10
MBN analysis: MBN Energy
MBN measurement of Q1N samples under stress
Stress levels: 0, 80, 160, 240, 320 and 400 MPa
  10
Minimum Y.S. = 550 MPa
Average of readings for five independent locations
(3 mm thick samples with 178 mm length and 33 mm width)

## Slide 11
Results
0 hr 48 hrs
96 hrs
168 hrs
336 hrs
Increasing tempering time
Reduction in pinning site density
  11

## Slide 12
Chart: Max Flux (T)
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
Q1 | 5.1197 | 16.5938 | 75.1492 | 142.549 | 199.249 | 243.612 | 284.476 | 339.123 | 376.074 | 398.831
Q2 | 6.2731 | 18.5152 | 93.6543 | 166.4528 | 202.186 | 216.4675 | 226.6483 | 234.715 | 236.8622 | 243.3105
Q3 | 6.606 | 25.1144 | 103.0441 | 165.3446 | 195.7714 | 210.6304 | 221.8808 | 226.9126 | 231.701 | 236.6254
Q4 | 4.8865 | 24.2579 | 112.439 | 169.388 | 194.4116 | 203.403 | 206.9988 | 209.9494 | 211.7578 | 215.0354
Q5 | 5.0019 | 20.9342 | 89.1283 | 137.0016 | 158.8324 | 166.87 | 171.839 | 177.399 | 179.2886 | 184.5824
Chart: MBN e
Q1 (0hr) | 398.8
Q2 (48 hrs) | 243.3105
Q3 (96 hrs) | 236.6254
Q4 (198 hrs) | 215.0354
Q5 (336 hrs) | 184.5824
Effect of microstructure (no applied stress) on MBN energy
1.0 Tesla
Greater tempering time:
  Increases degree of embrittlement
  reduces pinning site density in the matrix reduction in MBN signal
  Reason: Reduced interaction of 180° domain walls
  due to a decrease in available pinning sites
0 MPa
  12

## Slide 13
Chart: Q2 (48 hrs) RD
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
AVR f0 | 6.2731 | 18.5152 | 93.6543 | 166.4528 | 202.186 | 216.4675 | 226.6483 | 234.715 | 236.8622 | 243.3105
AVR f8 | 6.9962 | 37.8425 | 172.2715 | 247.656 | 273.069 | 278.0965 | 279.726 | 283.2368 | 281.4352 | 288.6315
AVR f16 | 7.4935 | 61.7396 | 244.33 | 317.6558 | 333.5955 | 334.7063 | 332.7185 | 330.233 | 332.1953 | 334.3043
AVR f24 | 7.5034 | 88.0503 | 305.493 | 376.9743 | 391.1045 | 384.5032 | 382.0362 | 379.542 | 378.7767 | 374.7288
AVR f32 | 5.5985 | 108.0707 | 366.034 | 430.6827 | 435.0233 | 427.7875 | 417.936 | 410.3537 | 403.0797 | 392.9495
AVR f40 | 7.2271 | 124.979 | 410.0557 | 478.3818 | 483.1135 | 469.2057 | 467.5563 | 459.7688 | 448.0025 | 438.3533
Chart: Q2 (48 hrs) TD
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
AVR f0 | 4.4599 | 7.109 | 29.5584 | 68.2234 | 104.6066 | 128.574 | 143.7608 | 156.6975 | 166.2312 | 171.3698
AVR f8 | 4.0726 | 5.4596 | 13.8467 | 32.6317 | 58.3198 | 78.5204 | 95.5926 | 110.1388 | 123.358 | 132.0195
AVR f16 | 4.268 | 5.1194 | 8.3918 | 16.8575 | 33.496 | 49.3197 | 64.0778 | 79.3334 | 94.7585 | 107.0165
AVR f24 | 4.2785 | 4.8783 | 6.5686 | 10.6683 | 20.8965 | 32.5044 | 44.371 | 57.8286 | 72.9397 | 84.8066
AVR f32 | 4.1605 | 4.5655 | 5.7975 | 8.1311 | 15.0034 | 23.6057 | 33.3501 | 44.9077 | 58.9465 | 69.9874
AVR f40 | 3.7056 | 4.0928 | 4.9859 | 6.5914 | 11.3571 | 18.0099 | 25.7533 | 35.8083 | 48.0985 | 58.5951
Effect of stress on MBN energy
Increasing stress level
0 MPa
0 MPa
400 MPa
400 MPa
  13
Notes: MBN energy increased with stress along the rolling direction (RD)
and decreased along the transverse direction (TD)

## Slide 14
Chart: Q5 (336 hrs) RD
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
AVR f0 | 5.0019 | 20.9342 | 89.1283 | 137.0016 | 158.8324 | 166.87 | 171.839 | 177.399 | 179.2886 | 184.5824
AVR f8 | 5.5882 | 39.6926 | 156.0016 | 213.1004 | 231.2518 | 235.3402 | 235.789 | 236.325 | 235.475 | 235.4076
AVR f16 | 5.6782 | 69.9109 | 223.259 | 275.4128 | 287.5784 | 284.023 | 282.6458 | 281.1364 | 276.9088 | 274.5614
AVR f24 | 5.9073 | 87.0788 | 273.9404 | 326.3388 | 334.1972 | 331.272 | 327.5848 | 322.716 | 320.9852 | 316.9554
AVR f32 | 5.8763 | 105.9021 | 324.7002 | 376.5058 | 385.4866 | 381.4056 | 375.953 | 368.9356 | 361.142 | 359.5252
AVR f40 | 6.0207 | 126.2501 | 380.6586 | 432.0348 | 437.2282 | 427.5188 | 421.0492 | 410.2874 | 402.6312 | 394.9544
Chart: Q5 (336 hrs) TD
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
AVR f0 | 3.5001 | 7.8567 | 39.9087 | 71.1586 | 96.3734 | 111.8598 | 121.3704 | 128.2284 | 133.8674 | 138.3232
AVR f8 | 3.6191 | 5.3144 | 16.669 | 38.1818 | 64.7873 | 84.954 | 99.3113 | 111.6716 | 122.7224 | 130.6038
AVR f16 | 4.5066 | 5.7046 | 9.4182 | 18.7949 | 36.7177 | 53.9739 | 69.2309 | 82.9862 | 96.7144 | 106.3039
AVR f24 | 3.4027 | 4.1427 | 5.8532 | 10.8343 | 23.0221 | 36.5821 | 49.7039 | 63.6175 | 77.7718 | 89.3465
AVR f32 | 3.2303 | 3.7441 | 4.7504 | 7.5942 | 15.8758 | 26.4123 | 37.2219 | 49.8207 | 63.9988 | 75.2149
AVR f40 | 3.2369 | 3.6029 | 4.4886 | 6.3383 | 11.941 | 19.7328 | 28.6403 | 39.7666 | 52.7586 | 64.2275
Reason: Increase in number of 180° domain walls with stress
and reduction in 90° domain volume
Increasing stress level
0 MPa
0 MPa
400 MPa
400 MPa
  14
Effect of stress on MBN energy
Notes: MBN energy increased with stress along the rolling direction (RD)
and decreased along the transverse direction (TD)

## Slide 15
Chart: Peak Flux (T)
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
Q1f0 | 5.1197 | 16.5938 | 75.1492 | 142.549 | 199.249 | 243.612 | 284.476 | 339.123 | 376.074 | 398.831
Q1f16 | 5.2277 | 39.7738 | 182.782 | 292.498 | 361.998 | 403.546 | 456.531 | 516.846 | 564.301 | 573.471
Q1f40 | 4.9455 | 69.1785 | 317.786 | 422.471 | 485.872 | 541.811 | 612.724 | 668.779 | 675.386 | 677.97
Q2f0 | 6.2731 | 18.5152 | 93.6543 | 166.4528 | 202.186 | 216.4675 | 226.6483 | 234.715 | 236.8622 | 243.3105
Q2f16 | 7.4935 | 61.7396 | 244.33 | 317.6558 | 333.5955 | 334.7063 | 332.7185 | 330.233 | 332.1953 | 334.3043
Q2f40 | 7.2271 | 124.979 | 410.0557 | 478.3818 | 483.1135 | 469.2057 | 467.5563 | 459.7688 | 448.0025 | 438.3533
Q3f0 | 6.606 | 25.1144 | 103.0441 | 165.3446 | 195.7714 | 210.6304 | 221.8808 | 226.9126 | 231.701 | 236.6254
Q3f16 | 6.5922 | 51.1679 | 212.898 | 301.7255 | 331.081 | 339.8168 | 337.3213 | 340.4798 | 336.5062 | 334.302
Q3f40 | 5.7329 | 84.314 | 358.6268 | 450.623 | 468.1235 | 457.8535 | 450.3785 | 438.8307 | 427.6248 | 419.459
Q4f0 | 4.8865 | 24.2579 | 112.439 | 169.388 | 194.4116 | 203.403 | 206.9988 | 209.9494 | 211.7578 | 215.0354
Q4f16 | 5.8629 | 86.4652 | 278.3548 | 343.3042 | 356.269 | 354.8122 | 350.6934 | 344.8302 | 339.8916 | 333.5898
Q4f40 | 6.5277 | 144.1378 | 425.6748 | 505.8084 | 513.3444 | 499.1958 | 493.6974 | 480.7362 | 461.173 | 455.6894
Combined effects of stress and microstructure on MBN energy
MBN energy along RD cannot be directly used to separate samples with different degrees of embrittlement under unknown levels of stress
  15
Notes: An indication of complexity of investigating simultaneous effects of stress and microstructural changes

## Slide 16
Chart: Peak Flux (T)
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
Q2f0 | 1.4065 | 2.6045 | 3.1685 | 2.4398 | 1.9328 | 1.6836 | 1.5766 | 1.4979 | 1.4249 | 1.4198
Q2f8 | 1.7179 | 6.9314 | 12.4413 | 7.5894 | 4.6823 | 3.5417 | 2.9262 | 2.5716 | 2.2815 | 2.1863
Q2f16 | 1.7558 | 12.0599 | 29.1152 | 18.8436 | 9.9593 | 6.7865 | 5.1924 | 4.1626 | 3.5057 | 3.1239
Q2f24 | 1.7537 | 18.0493 | 46.5083 | 35.3359 | 18.7162 | 11.8293 | 8.61 | 6.5632 | 5.193 | 4.4186
Q2f32 | 1.3456 | 23.6714 | 63.1368 | 52.9673 | 28.9949 | 18.1222 | 12.5318 | 9.1377 | 6.8381 | 5.6146
Q2f40 | 1.9503 | 30.5366 | 82.243 | 72.5765 | 42.5385 | 26.0527 | 18.1552 | 12.8397 | 9.3143 | 7.4811
Q3f0 | 1.6158 | 2.6804 | 2.1693 | 1.7924 | 1.5063 | 1.3751 | 1.3253 | 1.2612 | 1.2267 | 1.216
Q3f8 | 1.4835 | 6.1196 | 9.883 | 6.1412 | 3.7042 | 2.7701 | 2.2951 | 1.9995 | 1.7468 | 1.6146
Q3f16 | 1.7455 | 10.4796 | 25.5622 | 16.3993 | 7.9447 | 5.0766 | 3.7357 | 3.0309 | 2.483 | 2.1764
Q3f24 | 1.8451 | 16.8072 | 45.6559 | 32.1651 | 14.4791 | 8.4985 | 5.9032 | 4.3946 | 3.3961 | 2.8389
Q3f32 | 1.9218 | 23.4709 | 68.1796 | 51.6786 | 23.5973 | 12.8343 | 8.5497 | 6.08 | 4.5335 | 3.6882
Q3f40 | 1.8512 | 23.1704 | 77.8907 | 61.3153 | 32.3151 | 17.6253 | 11.8173 | 8.0245 | 5.8207 | 4.6664
Decoupling stress from microstructure
For 0.3 T, Ɵ shows most independency of the degree of embrittlement AND maximum sensitivity to the stress level
Samples with different degrees of
embrittlement have similar values
of Ɵ at a given stress
  16
Notes: Ɵ as a function of peak flux for samples experiencing different levels of temper embrittlement

## Slide 17
Chart: Stress (MPa)
| 0 | 80 | 160 | 240 | 320 | 400
Q2 | 3.2704 | 13.3928 | 27.798 | 48.7438 | 59.5555 | 87.06
Q3 | 2.1693 | 9.883 | 25.5622 | 45.6559 | 68.1796 | 77.8907
Q4 | 1.8978 | 7.5669 | 25.1688 | 47.1859 | 69.2016 | 88.6037
Q5 | 2.2333 | 9.3588 | 23.7051 | 46.8015 | 68.3516 | 84.8053
Q4 (surface2) | 3.1685 | 12.4413 | 29.1152 | 46.5083 | 63.1368 | 82.243
Effect of stress on Ɵ for samples with different degrees of temper embrittlement at 0.3 T
Sample | Q1 | Q2 | Q3 | Q4 | Q5
Heat treatment time (hr) at 525°C | 0 hr | 48 hrs | 96 hrs | 168 hrs | 336 hrs
Chart: Peak Flux (T)
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1
Q2f0 | 1.4065 | 2.6045 | 3.1685 | 2.4398 | 1.9328 | 1.6836 | 1.5766 | 1.4979 | 1.4249 | 1.4198
Q2f8 | 1.7179 | 6.9314 | 12.4413 | 7.5894 | 4.6823 | 3.5417 | 2.9262 | 2.5716 | 2.2815 | 2.1863
Q2f16 | 1.7558 | 12.0599 | 29.1152 | 18.8436 | 9.9593 | 6.7865 | 5.1924 | 4.1626 | 3.5057 | 3.1239
Q2f24 | 1.7537 | 18.0493 | 46.5083 | 35.3359 | 18.7162 | 11.8293 | 8.61 | 6.5632 | 5.193 | 4.4186
Q2f32 | 1.3456 | 23.6714 | 63.1368 | 52.9673 | 28.9949 | 18.1222 | 12.5318 | 9.1377 | 6.8381 | 5.6146
Q2f40 | 1.9503 | 30.5366 | 82.243 | 72.5765 | 42.5385 | 26.0527 | 18.1552 | 12.8397 | 9.3143 | 7.4811
Q3f0 | 1.6158 | 2.6804 | 2.1693 | 1.7924 | 1.5063 | 1.3751 | 1.3253 | 1.2612 | 1.2267 | 1.216
Q3f8 | 1.4835 | 6.1196 | 9.883 | 6.1412 | 3.7042 | 2.7701 | 2.2951 | 1.9995 | 1.7468 | 1.6146
Q3f16 | 1.7455 | 10.4796 | 25.5622 | 16.3993 | 7.9447 | 5.0766 | 3.7357 | 3.0309 | 2.483 | 2.1764
Q3f24 | 1.8451 | 16.8072 | 45.6559 | 32.1651 | 14.4791 | 8.4985 | 5.9032 | 4.3946 | 3.3961 | 2.8389
Q3f32 | 1.9218 | 23.4709 | 68.1796 | 51.6786 | 23.5973 | 12.8343 | 8.5497 | 6.08 | 4.5335 | 3.6882
Q3f40 | 1.8512 | 23.1704 | 77.8907 | 61.3153 | 32.3151 | 17.6253 | 11.8173 | 8.0245 | 5.8207 | 4.6664
0.3 T
Decoupling stress from microstructure
0.3 T
Strong correlation with applied uniaxial stress level
  17

## Slide 18
Conclusion
Decreasing MBN response with increasing temper embrittlement in Q1N samples
  due to reduced interaction of 180° domain walls with a decrease in available pinning sites
2. Increase in MBN energy with stress along RD and decrease along TD in Q1N samples
  due to increase of 180° domain walls in the direction of uniaxial tensile stress
3. MBN signals along RD has the ability to separate samples with different degree of embrittlement at zero stress
4. Combined effects of microstructural changes and applied uniaxial stress levels make it impossible to
correctly associates MBN signals with applied stress in Q1N samples experienced different levels of
temper embrittlement
5. The parameter Ɵ (the ratio of MBN energy in the RD to that in TD) at 0.3 Tesla was strongly
correlated with applied uniaxial stress level, independent of the degree of embrittlement of Q1N samples
  18

## Slide 19
Thank you
Questions?