## Slide 1: Towards a Practical Pulsed Eddy Current Inspection of Fasteners on Aircraft
P.R. Underhill, T.W. Krause
Royal Military College of Canada

## Slide 2
PEC Measurement
Practical Issues
Technical Issues
  Small signal in big scatter
  Cluster Analysis
Summary/Future Work
Outline
2

## Slide 3
No need to Remove Fasteners
Fast (3 seconds/measurement)
Why PEC?
3

## Slide 4
PEC Measurement
4
Take Physical Measurement
Convert Raw Data to Scores Using MPCA
Cluster Analysis
Check for Consistency

## Slide 5
Cluster Analysis
5
Cluster
ANN
Post Analysis | Post or Immediate
Requires a minimum number of measurements | Once trained can operate on single measurements
blind | Requires Training
No Calibration | Requires Calibration

## Slide 6
Cluster Analysis
6
Mahalnobis Distance
Need to know centroid and covariance matrix
Robust Statistics

## Slide 7
Practical Issues
7
Number fasteners
Check numbering
Data confirmation
Notes: Sound to check that measurement happened
Positioning system

## Slide 8
Technical Issues
8

## Slide 9
Technical Issues
9
2.5 mm crack
Fastener shift

## Slide 10
Technical Issues
10
Tilt 2.3 towards edge
Tilt 2.3 along Fasteners

## Slide 11
Partial Mahalanobis Distance
11
Scores 1 and 2
Scores 3 and 4

## Slide 12
Cut-off
12
(Robust MD)2

## Slide 13
Sample Size
13
Chart: Standard Deviations
| 2.1213203435596428 | 2.4041630560342475 | 2.6870057685088664 | 2.9698484809835 | 3.2526911934581046 | 3.5355339059327378 | 3.8183766184073571 | 1.8384776310850237 | 2.5455844122715714 | 2.8284271247461903 | 3.5355339059327378 | 3.5355339059327378 | 3.5355339059327378 | 3.5355339059327378
Simulation | 13 | 25 | 57 | 74 | 91 | 96 | 96 | 1 | 48 | 65 | 91 | 98 | 97 | 96
Logit fit | 0.1189 | 0.24709 | 0.51278 | 1.0611 | 2.183 | 4.4377 | 8.8114 | 16.7408 | 29.4974 | 46.541 | 64.4325 | 79.0336 | 88.6926 | 94.2268 | 97.1398 | 98.6047 | 99.3246 | 99.6743 | 99.8432 | 99.9246 | 99.9637 | 99.9826 | 99.9916 | 99.996 | 90

## Slide 14
Sample Size
14
Chart: Blank Samples
| 30 | 40 | 50 | 60 | 80 | 100
 | 3.91 | 3.61 | 3.23 | 2.94 | 2.81 | 2.81
Chart: Blank Samples
| 30 | 40 | 50 | 60 | 80 | 100
Average | 2.8137 | 1.877 | 1.5533 | 1.39 | 1.2544 | 1.1852
95% upper bound | 6.3947 | 3.8416 | 2.8003 | 2.42 | 1.9167 | 1.6931
a90
Slope of chi-square

## Slide 15
Twin Otter Layout
5
6
7
8
9
10
1
2
3
4
27
26
25
24
23
22
21
20
19
18
17
16
15
14
15

## Slide 16
Rotation by Repeat Measurement
16

## Slide 17
3D Visualization
17

## Slide 18
Need methods to link post analysis to fasteners under study
Demonstrated improved methodology for processing measurements
Some repeat measurements are useful to reduce scatter in visualization
Can’t handle isolated fasteners or small groups of fasteners
Summary
18

## Slide 19
ATESS
DTAES
Acknowledgements
19

## Slide 20
Questions?
20

## Slide 22
Outline
22