## Slide 1: Inspection Approaches for Lightning Damage to Composite Aircraft Structures
Catalin Mandache1, Marc Genest1, Behnam Ashrafi2
1 Structures and Materials Performance Laboratory
2 Aerospace Manufacturing Technologies Centre
Aerospace Research Centre • National Research Council Canada

## Slide 2: Outline
Lightning phenomena
Lightning and aircraft structures
Current inspection approaches
    Ultrasonic waves
    Radiography
Proposed inspection approaches
    Pulsed thermography
    Eddy current
    Capacitive imaging
  Summary and Conclusion
smithsonianmag.com

## Slide 3: Lightning phenomena
Lightning flash: overall lightning event, inter-cloud, between two clouds or between a cloud and the ground
    most common: inter-cloud, at 1.5-4.5 km altitude
    most intense: cloud-to-ground
Lightning strike: the attachment of the lightning flash to a structure (aircraft, building, wind turbine, etc.)
    it is estimated that a commercial airliner experiences a lightning strike every 1,000 to 3,000 flight hours
Rupke, 2002

## Slide 4: Lightning phenomena
Winter lightning – high intensity lightning flashes, at 0.5 km altitude
Sweers et al, 2021

## Slide 5: Lightning strikes effects on aircraft
Lightning strike effects:
Mechanic and Thermal:
Direct – due to the direct attachment of the lightning channel: bending, blasting, vaporization, punctures, fiber breakage
Electromagnetic:
Indirect – due to the fast rise or fall of electrical current: electromagnetic in nature
Lightning damage could be spotted at pre-flight walk-arounds
Sweers et al, 2021

## Slide 6: Lightning strikes and metallic structures
www.boeing.com
www.nypost.com
www.sciencefacts.net

## Slide 7: Composite structures requiring lightning strike protection (LSP)

## Slide 8: Lightning strikes and composite structures
smithsonianmag.com
Challenges:
multi-material
multi-layer
thin structure
anisotropic
smithsonianmag.com

## Slide 9: Lightning strike protection (LSP)
Materials:
Aluminum
Copper
Bronze
Nickel
Types:
Foils/Coatings
Straps
Meshes
    Expanded foils
    Interwoven
LSP Roles:
Provide a conductive path
Dissipate energy
Prevent structural damage
Prevent ignition of the fuel vapors
Electromagnetically shield aircraft navigation and avionics systems
Chemartin et al., 2012

## Slide 10: Experimental plan
Specimens:
Manufactured in-house at AMTC
1 ft x 1 ft panels (305 x 305-mm), 3.6 mm thick
Manufactured by hand layup, vacuuming and autoclaving
24 layers of unidirectional fibers, with a [45o/90o/- 45o/0o]3s layup configuration
Resin-embedded copper mesh added to the top-surface and co-cured with the composite panel
Aircraft grade priming and painting

## Slide 11: Experimental plan
Lightning impact:
Aircraft zoning
Lightning waveforms

## Slide 12: Lightning impact
National Testing Systems (NTS)/Lightning Technologies, Inc. in Pittsfield, MA
High-voltage (2.4 MV), high-current (>200 kA) generators
Capacitive banks

## Slide 13: Visual examination
Damage is supposed to be gradual, from P-1 to P-3 and include:
surface burn
damaged mesh
resin vaporization
fiber breakage
P-1
P-2
P-3
there is no damage on the back-side of the panels
Lightning damage could be spotted at pre-flight walk-arounds

## Slide 14: X-ray radiography
Computed radiography; local density changes affect the results.
source: 130 kV, 4 mA
exposure time: 20 sec
flexible plate resolution: 35 mm
P-1
P-2
P-3
It reveals mesh breakage and thinning of the panels

## Slide 15: Ultrasonic testing
Pulse-echo ultrasonic waves inspection from the back-side of the panels:
contact probe of 6.25 mm diameter
5 MHz frequency
0.5 mm resolution
water spray couplant
P-1
P-2
P-3
It reveals fibre breakage and delamination

## Slide 16: Infrared imaging
Imaging from the impacted side. Thermal conductivity and surface emissivity affect the results.
excitation with Xenon lamps of 4.8 kJ
long wave infrared camera (8-12 mm)
images represent the first derivative of temperature at 1 sec after flash excitation
P-1
P-2
P-3
Darker areas represent hotter (and thinner) regions

## Slide 17: Eddy currents
Scanning from the impacted side. It is sensitive to the electrical conductivity changes of the panels.
transmit/receive coaxial probe
15 kHz driving frequency
3 mm lift-off
0.5 mm resolution
P-1
P-2
P-3
Continuity of the Cu mesh is represented by the blue color.

## Slide 18: Capacitive imaging
Capacitor: a two-terminal device that stores electrical energy
Uses coplanar terminals
Senses the electric field disturbances

## Slide 19: Capacitive imaging
Scanning from the impacted side. It is sensitive to local dielectric constant changes.
5 V, 100 kHz sinusoidal waveform
0.5 mm resolution
5 mm lift-off
P-1
P-2
P-3
The indications represent areas of burnt Cu mesh

## Slide 20: Summary and Conclusion
Subsequent to lightning strikes, the extent of damage to the composite structure and the LSP material need to be precisely known in order to plan repairs
Radiographic and ultrasonic inspection techniques are effective, but require structural disassembly and significant aircraft downtime
Proposed techniques (thermography, eddy current, and capacitive imaging) do not require disassembly, are single-sided, and non-contact
      Infrared thermography is sensitive to material tinning
      Eddy current is sensitive to LSP discontinuity
      Capacitive imaging is sensitive to local dielectric changes
  Multi-technique data-fusion is currently underway

## Slide 21: THANK YOU
Dr. Catalin Mandache • Senior Research Officer • catalin.mandache@nrc-cnrc.gc.ca